|  |  | FLEXSTAR Assortment FLEXSTAR - District heating pipeline Composite system according to EN 15632 -1 /-2 suitable up to: max. 95°C (sliding) max. 80°C Continuous operating temperature max. 6 bar Operating pressure consisting of: Medium pipe made of cross-linked polyethylene (PEX) with oxygen diffusion barrier (EVOH) Insulation made of continuously produced CFC-free, flexible and longitudinally waterproof high-pressure polyurethane foam with the following thermal conductivities: FLEXSTAR:  ≤ 0.025 W/mK (≤ Ø 105 mm) Protective jacket made of an extremely sinusoidally corrugated, seamlessly extruded pol-yethylene (LLD-PE) including factory test Delivery on drums, in rings or as a set Single pipe FLEXSTAR-UNO Lfd. m FLEXSTAR 25/70 Lfd. m FLEXSTAR 32/70 Lfd. m FLEXSTAR 40/90 Lfd. m FLEXSTAR 50/90 Lfd. m FLEXSTAR 63/105 Ducting FLEXSTAR -DUO Lfd. m FLEXSTAR 25+25/90 Lfd. m FLEXSTAR 32+32/105 Lfd. m FLEXSTAR 40+40/125 Lfd. m FLEXSTAR 50+50/150 Connector (screw connection) For connection to continuing lines PEX connection piece (screw connection) made of brass with external thread suitable for: Piece PEX 25 mm Piece PEX 32 mm Piece PEX 40 mm Piece PEX 50 mm Piece PEX 63 mm Connecting piece (press connection) Made of brass with external thread suitable for: Piece PEX 25 mm Piece PEX 32 mm Piece PEX 40 mm Piece PEX 50 mm Piece PEX 63 mm Coupling (screw connection) Made of brass for connecting two FLEXSTAR heat pump pipes (without insulation material) suitable for: Piece PEX 25 mm on 25 mm Piece PEX 32 mm on 25 mm Piece PEX 32 mm on 32 mm Piece PEX 40 mm on 32 mm Piece PEX 40 mm on 40 mm Piece PEX 50 mm on 40 mm Piece PEX 50 mm on 50 mm Piece PEX 63 mm on 50 mm Piece PEX 63 mm on 63 mm Coupling (press connection) Made of brass / steel* for connecting two FLEXSTAR heat pump pipes (without insulation material) suitable for: Piece PEX 25 mm on PEX 25 mm Piece PEX 32 mm on PEX 25 mm Piece PEX 32 mm on PEX 32 mm Piece PEX 40 mm on PEX 32 mm Piece PEX 40 mm on PEX 40 mm Piece PEX 50 mm on PEX 40 mm Piece PEX 50 mm on PEX 50 mm Piece PEX 63 mm on PEX 50 mm Piece PEX 63 mm on PEX 63 mm Elbow 90° (press connection) Made of brass or steel for connecting two FLEXSTAR heat pump pipes (without insulation material) suitable for: Piece PEX 25 mm* Piece PEX 32 mm* Piece PEX 40 mm* Piece PEX 50 mm* Piece PEX 63 mm* * Post-insulation with L or Big-L - clip shells * Post-insulation with Big-L clip shells Shrink-on end cap for damp locations Heat-shrinkable, as termination for house entries, consisting of: Molecularly cross-linked and modified polyolefin coated with sealing adhesive. (Temperature resistant up to 125 °C) Incl. temperature gauge and abrasive belt. Shrink-on end cap for FLEXSTAR -UNO suitable for: Piece FLEXSTAR 25/70 Piece FLEXSTAR 32/70 Piece FLEXSTAR 40/90 Piece FLEXSTAR 50/90 Piece FLEXSTAR 63/105 Shrink-on end cap for FLEXSTAR -DUO Piece FLEXSTAR 25+25/90 Piece FLEXSTAR 32+32/105 Piece FLEXSTAR 40+40/125 Piece FLEXSTAR 50+50/150 End cap for drying rooms As a closure for house furnishings, consisting of: PE-LD push-on cap End cap for FLEXSTAR -UNO Piece FLEXSTAR 25/70 Piece FLEXSTAR 32/70 Piece FLEXSTAR 40/90 Piece FLEXSTAR 50/90 Piece FLEXSTAR 63/105 End cap for FLEXSTAR-DUO Piece FLEXSTAR 25+25/90 Piece FLEXSTAR 32+32/105 Piece FLEXSTAR 40+40/125 Piece FLEXSTAR 50+50/150 Sealing ring Consisting of a specially profiled neoprene ring suitable for: Piece Outer pipe 70 mm Piece Outer pipe 90 mm Piece Outer pipe 105 mm Piece Outer pipe 125 mm Piece Outer pipe 150 mm Rentable tool for press connectors Dimensions: ø 20 - 40 mm (heating / sanitary) Tool for dimensions ø 20 - 40, consisting of: Tool case, expanding tool and pressing tool 1 Set Rentable tool set for press connectors Dimensions: ø 50 - 110 mm Set consisting of 2 tool cases 1 tool case with expanding tool ø 50 - 110 1 tool case with grouting tool ø 50 - 110 both tool cases are necessary 1 Set |  |  |
| --- | --- | --- | --- | --- |